Supporting Information

Enhanced Photocatalytic CO2 Reduction Performance in Ni-Doped Perovskite Nanocrystals Controlled by Magnetic Fields

S1 Schematic diagram of catalyst synthesis device.

Figure S1 Schematic diagram of catalyst synthesis device.

S2 Schematic diagram of photocatalytic reaction with a magnetic field.

Figure S2 Schematic diagram of photocatalytic reaction with a magnetic field.

S3 XPS of Ni-CsPbCl3 with a doping ratio of 8.0 at. %.

Figure S3 XPS of Ni-CsPbCl3 with a doping ratio of 8.0 at. %.

S4 The product yields of Ni-CsPbCl3 with various Ni doping ratios in an argon atmosphere.

Figure S4 The product yields of Ni-CsPbCl3 with various Ni doping ratios in an argon atmosphere.

S5 Tauc Plot of the catalysts. The method for obtaining Tauc Plot by UV-VIS absorption mapping: Convert the wavelength (𝜆) to photon energy (ℎ𝜈) using the relation: hν= hc/ 𝜆. Plot (Aℎ𝜈)𝑛 on the y-axis against hν on the x-axis. The optical band gap (𝐸𝑔) is determined by extrapolating the linear portion of the Tauc plot to the x-axis (where (Aℎ𝜈)𝑛 =0). The intercept on the x-axis gives the band gap energy.

Figure S5 (a) Tauc Plot of CsPbCl3, Ni-CsPbCl3 with a doping ratio of 8.0 at. % and (b) Ni-CsPbCl3 with a doping ratio of 9.1 at. %.

Figure S6 XRD of Ni-CsPbCl3 with a doping ratio of 8.0 at. % and Ni-CsPbCl3 with a doping ratio of 9.1 at. %.

Figure S6 XRD of Ni-CsPbCl3 with a doping ratio of 8.0 at. % and Ni-CsPbCl3 with a doping ratio of 9.1 at. %.

Figure S7 XRD of CsPbCl3 before and after reaction.

Figure S7 XRD of CsPbCl3 before and after reaction.

Table S1 Atomic doping ratio corresponding to each feeding ratio.

| Feed ratio (molar ratio) | Ni doping ratio (at. %) |
| --- | --- |
| 1:1 | 0.9 |
| 2:1 | 4.8 |
| 3:1 | 5.8 |
| 4:1 | 8.0 |
| 5:1 | 9.1 |

Table S2 Summary of the photocatalytic CO2 reduction performance of perovskite.

| Photocatalyst | Reaction medium (Reaction system) | Products and Yield (μmol g-1h-1) | Stability time (h) | Refs |
| --- | --- | --- | --- | --- |
| Ni-CsPbCl3 （500mT） | CO2/H2O vapor (solid–gas) | CO:27.3 | 36 | This work |
| Ni-CsPbCl3 | CO2/H2O vapor (solid–gas) | CO: 3.8 | 36 | This work |
| Cs4Pb3Br10 Cs5Pb4Br13 | CO2/H2O vapor (solid–gas) | CO: 9.14, CH4: 0.7 CO:13.57, CH4: 0.64 | 30 | [1] |
| Mn-CsPbBr3 NPLs | CO2/H2O vapor (solid–gas) | CO: 7.56, CH4: 0.58 | 24 | [2] |
| Cu: CsPbBr3 | CO2/H2O vapor (solid–gas) | CO: 0.53 ± 0.08, CH4: 14.72 ± 0.60 | 5 | [3] |
| CsPbBr3/Pd | CO2/H2O vapor (solid–gas) | CO: 5.77, CH4: 10.41, H2: 3.29 | 3 | [4] |

Reference

[1]	Lin C-C, Li J-Y, She N-Z, et al., Stabilized High-Membered and Phase-Pure 2D All Inorganic Ruddlesden–Popper Halide Perovskites Nanocrystals as Photocatalysts for the CO2 Reduction Reaction. Small, 2022, 18 (19): 2107881.

[2]	Lin C-C, Liu T-R, Lin S-R, et al., Spin-Polarized Photocatalytic CO2 Reduction of Mn-Doped Perovskite Nanoplates. J Am Chem Soc, 2022, 144 (34): 15718-15726.

[3]	Bian H, Liu T, Li D, et al., Unveiling the effect of interstitial dopants on CO2 activation over CsPbBr3 catalyst for efficient photothermal CO2 reduction. Chem Eng J, 2022, 435: 135071.

[4]	Xu Y-F, Yang M-Z, Chen H-Y, et al., Enhanced Solar-Driven Gaseous CO2 Conversion by CsPbBr3 Nanocrystal/Pd Nanosheet Schottky-Junction Photocatalyst. ACS Appl Energy Mater, 2018, 1 (9): 5083-5089.