Supporting Information

Effect of substrate temperature and oxygen plasma treatment on the property of magnetron sputtered CdS for solar cell applications

Figure S1. The overall experimental procedure and device structure. a) CdS sputtering and annealing process b) Sb2(S,Se)3 thin film hydrothermal growth, HTL and electrode deposition process.

Supplementary Note 1. The advantage of magnetron sputtered CdS mentioned in the main text are explained in detail here.

1. Higher environmental friendliness. Traditional CBD methods uses a solution that contains Cd ions and ammonia as the reacting solution. Preparing 12 pieces of CdS thin film with the size of 1.5×2 cm would produce about 150 ml of wastewater. Though the concentration of Cd ion in the solution is relatively low (about 0.01 mol/L), special treatment must be conducted before these wastewater can be dumped into the water drainage system. The concentration of Cd ions must be lower than 0.01 mg/L as irrigation water due to the toxicity of Cd ions. Producing solar cell module with size of about 1 m2 would produce about 42 L of wastewater. Such amount of wastewater would be a huge economic and environmental problem in the manufacturing process. However, the magnetron sputtering uses target as the source, which produces no waste at all. The manufacture of target itself is also environmentally friendly since only CdS powder is used as the ingredient. Therefore, magnetron sputtering process is much more environmental friendly.

2. Good control of film thickness. The deposition rate of traditional CBD methods depends on the environment. Change of ambient temperature and humidity and the unavoidable fluctuation of concentration of ammonia solution would all lead to a different thin film deposition rate. However, since the sputtering process is carried out in a vacuum environment, all of the environment parameters can be controlled. Therefore a more accurate film thickness can be achieved

3. High uniformity on large size substrate. Recently, solar cell giant agree that the standard size of Si solar cell module should be 2382×1134 mm. In order to improve the commercial viability of solar cell, techniques with the ability to deposit thin film on such a large size must be developed. Previous patent shows the size of magnetron sputtered target can reach the size of several square meters[1-2], which is suitable for the production of solar cell module. However, reports of the largest CdS fabricated using CBD method is only 30×40 cm, which is smaller than the current standard Si solar cell module size. In addition, the uniformity of thin film prepared by magnetron sputtered is higher. Previous result shows that thickness deviation over is about 2.8% while deviation is about 20%[3-4]. Therefore, magnetron sputtering is a more suitable thin film deposition technology for depositing CdS window layer in future Sb2(S,Se)3 solar cell module manufacture.

Figure S2. XRD pattern of CdS sputtered on glass. The sputtering time is the standard time used in the device fabrication (29 minutes). Signals were smoothed using 10 points adjacent-averaging method. Main peaks can still be found, but noise make recognition of the peaks difficult.

Figure S3. SEM image of CdS sputtered on FTO at RT condition without post annealing. The sputtering time is 4 times the standard time. a) Surface of CdS, b) Cross sectional view of CdS. Under such a long sputtering time, the morphology of FTO substrate can no longer be seen. The thickness of this CdS thin film is measured to be around 240 nm, so the thickness of CdS used in the device is around 60 nm.

Figure S4. SEM image of CdS sputtered at different time scale. a) 1/4 full time, b) 1/2 full time, c) 3/4 full time and d) full time.

Supplementary Note 2. In order to know the growth process of CdS film using magnetron sputtering method, SEM top view images were taken at different growth time (Figure 3e-h). It can be seen that at the ¼ of the full film growth time, little CdS nanoparticles can be barely seen on the FTO substrate. At ¾ of the full film growth time, the morphology is similar to the film grown full time. The difference is that the size of CdS nanoparticles is larger in the full time growth film than the ¾ growth time film. The first step of the sputtering process is the decomposition of compound caused by bombardment of Ar ion. Excitation and ionization may also occur in this process.[5-6] In this process, the decomposed particles may exists in CdS cluster form or Cd atom and S atom form. Then particles of composite element flew to the substrate. Finally, particles recombine together at the substrate surface.

Figure S5. AFM image of CdS sputtered at different substrate heating condition. a) RT, b) 150 ℃, c) 200 ℃ and d) 250 ℃.

Figure S6. Illustration of sputtering result of CdS thin film. Under substrate heating condition, the crystallinity of the thin film increases and the surface roughness decreases.

Figure S7. UV-Vis result of Sputtered CdS thin film on FTO substrate. a) The original absorbance result. b) The tauc plot of the UV-Vis result. As a direct bandgap material, the absorption coefficient and the bandgap Eg has the relation

(αhν)2=A(hν-Eg)                            (2)

where α is the absorption coefficient, h is the Planck constant, υ is the frequency of the incident photon, A is a proportionality constant, and Eg is the bandgap value. By extrapolating the linear part of (αhν)2 using hν as the x-axis, the bandgap of CdS can be derived. The bandgap value for RT, 150 ℃, 200 ℃ and 250 ℃ CdS are 2.34 eV, 2.35 eV, 2.35 eV and 2.35 eV respectively. The bandgap of CdS sputtered under different substrate heating condition is similar after CdCl2 spin coating and ambient air annealing process.

Figure S8. SEM image of Sb2(S,Se)3 thin film. a) Grown on CBD CdS substrate. b) Grown on sputtered CdS at 150 ℃ condition. c) Grown on sputtered CdS at 250 ℃ condition. SEM image of Sb2(S,Se)3 thin film grown on RT and 200 ℃ condition sputtered CdS are shown in the main text (Figure 3).

Figure S9. Statistical analysis of the grain size distribution of Sb2(S,Se)3 thin film grown on CBD CdS substrate. The average grain size is a slightly smaller than Sb2(S,Se)3 thin film grown on sputtered CdS at 200 ℃ condition (Figure 3b, 537 nm compared with 597 nm).

Figure S10. Bandgap of Sb2(S,Se)3 grown on RT sputtered CdS. The result is calculated based on EQE data.[7] The y axis is [Eln(1-EQE)]2, following the tauc plot rule.

Figure S11. Cross-sectional SEM image of Sb2(S,Se)3 solar cell.

Table S1. Electrochemical impedance spectroscopy (EIS) result Sb2(S,Se)3 solar cell device grown on sputtered CdS under different heating condition.

| Condition | Rs (Ω) | Rrec (Ω) |
| --- | --- | --- |
| RT | 34.0 | 2736 |
| 150 ℃ | 45.4 | 13507 |
| 200 ℃ | 8.3 | 128580 |
| 250 ℃ | 24.3 | 51232 |

Figure S12. Statistical boxplot of a) series resistance and b) shunt resistance of Sb2(S,Se)3 solar cell devices grown on sputtered CdS under different substrate heating condition. All these data are provided by the solar cell measurement software based on J-V data under illumination condition.

Figure S13. a) TAS mappings of Sb2(S,Se)3 thin films deposited on Sputtered CdS at 150 ℃ condition. b) Original data and fitted curves of transient decay kinetics monitored at 665 nm for Sb2(S,Se)3 films grown on sputtered CdS at 150 ℃ and 250 ℃ condition. c) Fitted curves of transient decay kinetics monitored at 665 nm for Sb2(S,Se)3 films grown on sputtered CdS at all four condition. All the calculated average lifetime is shown in the graph.

Figure S14. a) EQE spectrum of five different antimony chalcogenide solar cell. Sb2S3, SU Sb2(S,Se)3 and SSS Sb2(S,Se)3 are all fabricated using hydrothermal method. SU means selenourea.[8] SSS means sodium selenosulfate.[9] TE means thermal evaporation.[10] MBE means molecular beam epitaxy. The Se/S ratio near the CdS layer of SU Sb2(S,Se)3 is larger than that of SSS Sb2(S,Se)3 though the overall Se/S ratio in the whole absorber layer of SSS Sb2(S,Se)3 is larger. b) Short wavelength EQE spectrum of device with different oxygen plasma treatment condition. c) Full wavelength EQE spectrum of device with different oxygen plasma treatment condition. The integrated current density based on EQE data are shown in the figure. The trend of integrated current density matches well with the statistics of J-V result.

Figure S15. Statistical boxplot of Sb2(S,Se)3 solar cell device parameter with different oxygen plasma treatment conditions. a) Power conversion efficiency (PCE), b) JSC, c) FF and d) VOC.

Figure S16. EQE spectra of Sb2(S,Se)3 solar cell device based on sputtered CdS with and without oxygen plasma treatment (OPT). a) RT condition, b) 150℃ condition and c) 250℃ condition. EQE spectra of 200℃ condition is shown in the main text (Figure 9e). Under all the sputtering condition, oxygen plasma treatment improve the EQE response at short wavelength (<520nm).

Figure S17. UV-vis result of sputtered CdS before and after oxygen plasma treatment (OPT). a) The original transmission result. b) The tauc plot of the UV-Vis result.

Figure S18. Statistical boxplot of device performance with and without oxygen plasma treatment.

Figure S19. SEM image of sputtered CdS after CdCl2 spin coating and ambient air annealing. a) Without oxygen plasma treatment. b) With 15 minutes oxygen plasma treatment. c) With 30 minutes oxygen plasma treatment. EDS result of these CdS thin film is shown in the main text (Figure 9i). As the oxygen plasma treatment time extends, the original morphology is changed. For 30 minutes condition, the FTO substrate can be barely recognized.

Figure S20. XPS spectra of S 2p orbit in both control CdS and OPT CdS.

Figure S21. Water contact angle of sputtered CdS after CdCl2 spin coating and ambient air annealing. a) Without oxygen plasma treatment. b) With 15 minutes oxygen plasma treatment. Theoretically, a smaller contact angle results in lower Gibbs free energy for heterogeneous nucleation, thereby increasing the nucleating density and promoting the film densification process.[11]

Figure S22. Statistical boxplot of Sb2(S,Se)3 solar cell device parameter with cadmium chloride spin coating. a) Power conversion efficiency, b) JSC, c) VOC and d) FF. The unit is mg/ml. Note that in all these device CdS was treated by oxygen plasma.

Figure S23. Statistical boxplot of Sb2(S,Se)3 solar cell device parameter with mixed chloride (CdCl2+SbCl3) spin coating. a) Power conversion efficiency, b) JSC, c) FF and d) VOC. The number before the “+” sign means the CdCl2 concentration, while the number after the “+” sign means the SbCl3 concentration. The unit is mg/ml. The optimal concentration of SbCl3 used in CBD CdS for Sb2Se3 device is 30mg/ml in reference.[10]

Supplementary Note 3. Chloride treatment is a beneficial way to passivate the grain boundary defects in different kinds of solar cells.[10, 12-22] The standard protocol of Sb2(S,Se)3 solar cell device fabrication includes CdCl2 spin coating treatment of CdS layer before ambient air annealing.[8] In previous report, another chloride, SbCl3,[10] was used to treat CdS in the thermal evaporated Sb2Se3 device. A smoother surface can be formed by using SbCl3 treatment. Herein, a mixture of CdCl2 and SbCl3 is used as another method to improve the quality of sputtered CdS thin film and the device performance. As can be seen from the statistical plot (Figure S22), the VOC of device using mixed chloride treatment shows a slight increase. This can also be evidenced by the increase in built-in electric field from C-V test (Figure S24). The UV-Vis result shows an increase in transmission of CdS thin film, much higher than the oxygen plasma treatment (Figure S25). The increase in transmission might be the origin of increase in PCE and VOC.

Figure S24. SEM image of sputtered CdS after CdCl2 and SbCl3 mixed chloride solution spin coating and ambient air annealing. a) Without oxygen plasma treatment. b) With 15 minutes +15 minutes oxygen plasma treatment. With the existence of SbCl3, the CdS does not undergo a shape reform after ambient air annealing. The morphology of FTO substrate can be clearly seen.

Figure S25. The 1/capacitance2–voltage (1/C2–V) curves of the devices with different chloride spin coating condition. The data was recorded at a frequency of 100 kHz at room temperature in dark.

Figure S26. a) UV-Vis result of Control and Dual Chloride Spin-Coating (DCSC) treated CdS. b) difference in transmission rate between OPT and control and DCSC and control.

Figure S27. Champion device J-V curve of Sb2(S,Se)3 solar cell device grown on sputtered CdS under the optimal condition and CBD CdS.

Figure S28. EQE spectra of champion Sb2(S,Se)3 solar cell device based on sputtered CdS with both oxygen plasma treatment (OPT) and dual chloride spin coating (DCSC) post treatment. The calculated current density is 20.93 mA cm-2, which is close to the JSC measured from J-V curve.

Table S2. Champion device parameter of Sb2(S,Se)3 solar cell device grown on sputtered CdS under the optimal condition and CBD CdS.

| Condition | Voc (mV) | Jsc (mA cm-2) | FF (%) | η (%) |
| --- | --- | --- | --- | --- |
| Sputtered CdS | 643 | 20.67 | 60.89 | 8.09 |
| CBD CdS | 643 | 20.97 | 66.34 | 8.94 |

Table S3. Comparison of PCE between different antimony selenosulfide solar cells based on sputtered CdS.[23-26]

| Journal | Year | Device structure | Voc/V | Jsc/mA cm-2 | FF/% | PCE/% |
| --- | --- | --- | --- | --- | --- | --- |
| Applied Materials Today | 2019 | Glass/ITO/Sputtered CdS/Sb2Se3/Au | 0.379 | 27.93 | 55.6 | 5.91 |
| Journal of Alloys and Compounds | 2022 | Glass/Mo/MoSe2/Sb2Se3/CBD CdS/Sputtered CdS:O/ZnO/AZO | 0.408 | 28.11 | 66.98 | 7.69 |
| Solar Energy Materials and Solar Cells | 2019 | Glass/FTO/SnO2/Sputtered CdS:O/Sb2Se3/Spiro-OMeTAD/Au | 0.394 | 27.2 | 58.7 | 6.29 |
| Solar RRL | 2019 | Glass/FTO/Sputtered CdS:O/ Sb2Se3/graphite/Ag | 0.432 | 29.87 | 54 | 7.01 |
| This work |  | Glass/FTO/Sputtered CdS/Hydrothermal Sb2(S,Se)3/Spiro-OMeTAD/Au | 0.643 | 20.67 | 60.89 | 8.09 |

References

[1]	M. E. Gaydos, P. Kumar, S. Miller, et al.  Patent US2006040214, 2006.

[2]	L. F. Mchugh, P. Kumar, D. Meendering, et al.  Patent US2004020932, 2004.

[3]	C. Fu, C. Yang, L. Han, et al. The thickness uniformity of films deposited by magnetron sputtering with rotation and revolution. Surface and Coatings Technology, 2006, 200(12): 3687-3689.

[4]	Y. Cai, W. Li, L. Feng, et al. Preparation and properties of CdS thin films with large area. Journal of Sichuan University (Natural Science Edition), 2008, 45(2): 387-390.

[5]	H. Adachi, T. Hata, T. Matsushima, et al., Handbook of Sputter Deposition Technology, Elsevier, USA 2012.

[6]	H. H. Andersen, H. L. Bay, R. Behrisch, et al., Sputtering by Particle Bombardment I, Springer, Germany 1981.

[7]	Y. Sun, P. Qiu, W. Yu, et al. N‐Type Surface Design for p‐Type CZTSSe Thin Film to Attain High Efficiency. Advanced Materials, 2021, 33(49): 2104330.

[8]	R. Tang, X. Wang, W. Lian, et al. Hydrothermal deposition of antimony selenosulfide thin films enables solar cells with 10% efficiency. Nature Energy, 2020, 5(8): 587-595.

[9]	J. Dong, H. Liu, Z. Cao, et al. Low‐Cost Antimony Selenosulfide with Tunable Bandgap for Highly Efficient Solar Cells. Small, 2022, 19(9): 2206175.

[10]	H. Cai, R. Cao, J. Gao, et al. Interfacial Engineering towards Enhanced Photovoltaic Performance of Sb2Se3 Solar Cell. Advanced Functional Materials, 2022, 32(46): 2208243.

[11]	J. Li, Y. Zhao, C. Li, et al. Hydrazine Hydrate‐Induced Surface Modification of CdS Electron Transport Layer Enables 10.30%‐Efficient Sb2(S,Se)3 Planar Solar Cells. Advanced Science, 2022, 9(25): 2202356.

[12]	Y. Dong, L. Huang, H. Wang, et al. Zinc Chloride‐Treated Indium Sulfide as Buffer Layer for Cd‐Free Antimony Selenide Solar Cells. Solar RRL, 2023, 7(18):

[13]	B. Ghosh, M. Das, P. Banerjee, et al. Fabrication of vacuum-evaporated SnS/CdS heterojunction for PV applications. Solar Energy Materials and Solar Cells, 2008, 92(9): 1099-1104.

[14]	N. R. Paudel, M. Young, P. J. Roland, et al. Post-deposition processing options for high-efficiency sputtered CdS/CdTe solar cells. Journal of Applied Physics, 2014, 115(6): 064502.

[15]	I. Riech, J. L. Peña, O. Ares, et al. Effect of annealing time of CdCl2 vapor treatment on CdTe/CdS interface properties. Semiconductor Science and Technology, 2012, 27(4): 045015.

[16]	L. Wang, M. Luo, S. Qin, et al. Ambient CdCl2 treatment on CdS buffer layer for improved performance of Sb2Se3 thin film photovoltaics. Applied Physics Letters, 2015, 107(14): 143902.

[17]	W. Xia, H. Lin, H. N. Wu, et al. Effects of high-temperature annealing on ultra-thin CdTe solar cells. Thin Solid Films, 2011, 520(1): 563-568.

[18]	G. Zeng, P. Harrison, A. Kidman, et al. Correlation of microscopic grain evolution in post‐CdCl2 annealing and performance of CdS/CdTe thin‐film solar cells fabricated using pulsed laser deposition. physica status solidi (a), 2016, 213(12): 3231-3237.

[19]	J. Zhou, X. Zhang, H. Chen, et al. Dual-function of CdCl2 treated SnO2 in Sb2Se3 solar cells. Applied Surface Science, 2020, 534(1): 147632.

[20]	Y. Zhou, L. Wang, S. Chen, et al. Thin-film Sb2Se3 photovoltaics with oriented one-dimensional ribbons and benign grain boundaries. Nature Photonics, 2015, 9(6): 409-415.

[21]	L. Huang, J. Yang, Y. Xia, et al. InCl3-modified SnO2 as an electron transporting layer for Cd-free antimony selenide solar cells. Journal of Materials Chemistry A, 2023, 11(32): 16963-16972.

[22]	B. Dahal, R. Guo, R. Pathak, et al. Enhancing the performance of the perovskite solar cells by modifying the SnO2 electron transport layer. Journal of Physics and Chemistry of Solids, 2023, 181(1): 111532.

[23]	L. Guo, B. Zhang, S. Ranjit, et al. Interface Engineering via Sputtered Oxygenated CdS:O Window Layer for Highly Efficient Sb2Se3 Thin‐Film Solar Cells with Efficiency Above 7%. Solar RRL, 2019, 3(10): 1900225.

[24]	X. Hu, J. Tao, Y. Wang, et al. 5.91%-efficient Sb2Se3 solar cells with a radio-frequency magnetron-sputtered CdS buffer layer. Applied Materials Today, 2019, 16(1): 367-374.

[25]	Y. Liu, B. Li, X. Liang, et al. Reactively sputtered CdS:O buffer layers for substrate Sb2Se3 solar cells. Journal of Alloys and Compounds, 2023, 932(1): 167313.

[26]	C. Ou, K. Shen, Z. Li, et al. Bandgap tunable CdS:O as efficient electron buffer layer for high-performance Sb2Se3 thin film solar cells. Solar Energy Materials and Solar Cells, 2019, 194(1): 47-53.